Barton Cutting Oil

Excelfluid FSLF

Fully synthetic biostable metalworking fluid

Product Description:

Excelfluid FSLF is a fully synthetic water-mix cutting fluid that forms a true solution when diluted with water. It provides superior cooling and flushing characteristics, whilst providing excellent swarf settlement characteristics.

Excelfluid FSLF provides excellent corrosion protection on both the machine tool and components whilst minimising the build-up of sticky residues and maintaining excellent machine tool cleanliness.

Excelfluid FSLF is based upon high performance anti-corrosion additives in order to provide excellent residual corrosion protection of the machine tool and machined components alike. It produces a transparent solution which allows for excellent visibility for the machine operator and has an ultra-low foaming tendency making it suitable for the most arduous modern day machining requirements.

Benefits

- Ultra low foaming

- Chlorine free

- Secondary amine free

- Triazine free

- High levels of lubrication

- Excellent swarf settlement

- Long sump life

Application

Excelfluid FSLF is able to cope with materials with widely differing machining characteristics, including cast iron and mild steel. Excelfluid FSLF is particularly suited to CNC machining while also being suitable for more arduous grinding operations, particularly where high pressures and agitation are involved.

| Typical Test Data |  |  |
| --- | --- | --- |
| Appearance of Concentrate | Amber liquid |  |
| Odour | Bland |  |
| Emulsion Appearance | Transparent solution |  |
| Specific Gravity @ 20°C | 1.080 |  |
| pH @ 5% (Distilled Water) | 9.3 |  |
| Anti-Corrosion by IP 287 | 2% break point |  |
| Reichert Lubricity Performance | Noise Reduction 15m |  |
| @ 10% Dilution | Load Capacity 1.95Kg/mm2 |  |
| Refractometer Factor | 2.2 |  |

# Text boxes

BARTON

LUBE