DATA SHEET

Cyclone Turbine Range

Mineral oil based turbine oils

Product Description:

The Cyclone Turbine range is manufactured from the highest quality solvent refined mineral base oil fortified with a proprietary turbine oil additive.

The state of the art additive system offers outstanding protection against oxidation, gives long-term corrosion protection, and helps retain good oil demulsibility in the presence of water.

Benefits:

- Excellent oxidation stability

- Superior demulsification in the presence of water

- Long term corrosion protection

Application:

Turbine oil has a number of vital functions to perform. It must lubricate and cool the turbine and generator bearings, couplings and reduction gears as well as protect the system from rust, corrosion, and oxidation. The use of Cyclone Turbine oils ensures that all of these needs are met and exceeded.

|  | Performance Specifications: |  |  |
| --- | --- | --- | --- |
|  | ASTM | D-4304 Type I & Type III |  |
|  | Alstom | HTGD 90117 |  |
|  | British Standard | BS 489 |  |
|  | Denison | HF-1 |  |
|  | Cincinnati Milacron | P-38 (ISO 32), P-54 (ISO 68), |  |
|  |  | P-55 (ISO 46) & P-57 (ISO 150) |  |
|  | DIN | 51524 Part 1 |  |
|  |  | 51515 Part 1: L-TD & Part 2: L-TG |  |
|  | General Electric | GEK-32568F |  |
|  |  | 8068 L-TGB & L-TGSB |  |
|  | ISO | 6743-5 L-TSA & L-TGA |  |
|  |  | 11158 HH & HL |  |
|  | US Steel | 120 & 126 |  |
|  | Military | MIL-L-17672 C |  |
|  | AFNOR | E-48600 HL |  |
|  | Siemens AG | TLV 9013 04 (Standard Thermal Stability) |  |
|  |  | TLV 9013 05 (High Thermal Stability) |  |
|  | Brown Boveri | HTGD 90117 |  |

DATA SHEET

Typical Test Data:

| Cyclone Turbine | 32 | 46 | 68 | 100 | 150 | 220 | 320 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Product Code | C011 | C018 | C012 | C015 | C013 | C017 | C042 |
| ISO VG | 32 | 46 | 68 | 100 | 150 | 220 | 320 |
| Specific Gravity @ 15.6°C | 0.873 | 0.878 | 0.884 | 0.889 | 0.890 | 0.893 | 0.895 |
| Kinematic Viscosity @ 40°C (cSt) | 30.5 | 46.1 | 67.1 | 100.1 | 148.3 | 223.7 | 317.9 |
| Viscosity Index | 102 | 102 | 104 | 100 | 100 | 101 | 99 |
| Flash Point (°C) | 215 | 220 | 235 | 225 | 230 | 235 | 237 |

Health & Safety:

Please refer to the safety data sheet, a copy of which is freely available to all of our customers.